| SPECIFICATION TEXT |  |  |  |
| --- | --- | --- | --- |
| PRODUCT | Durelis StormBlock | DATE | 11/06/2015 |
| CE CLASS | P5 | EN STANDARD | EN 312 |

DESCRIPTION

Moisture-repellent, vapour permeable structural construction board with high air-tightness

Durelis StormBlock is a construction board belonging to product class P5 (standard reference EN 312): panels for load-bearing applications for use in humid conditions and in hazard classes of biological attack 1 and 2 of EN 335-3. These panels are therefore in the same area of application as OSB/3 (EN 300), multiplex (EN 636-2).

In timber-frame constructions and low-energy and passive house buildings, Durelis StormBlock can be used as a reinforcing exterior wall, as part of a façade or as a partition wall. When used as a façade element, Durelis StormBlock must be protected with a rain screen.

Durelis StormBlock is an MUF bonded chipboard with a TopFinish surface. This TopFinish surface provides very high air-tightness (< 0.0025 m³/ m²/h/Pa at 50 Pa; 15 mm). It is important always to seal all joints and gaps with suitable air-tight tape. The composition of construction board limits linear expansion and swelling to a minimum in high air humidity conditions.

On delivery and as much as possible during and after installation, the panels should be well protected against any direct contact with water. They must be stacked flat on a pallet or sufficient number of cross beams. Panels are not stored vertically unless ground contact can be avoided. The panels will expand/contract under the influence of variable humidity conditions so room to expand must always be provided. Use suitable tools for sawing, milling and drilling. Nails or screws must not be inserted within a minimum 8 mm of the edge of the panel.

STANDARD DIMENSIONS

Standard dimension: 2,800 x 1,196 x 12 mm (H x W x D)

Various thicknesses and lengths/widths for compressing and finishing can be discussed. Contact our agent about this or send an email to info.panels@unilin.com.

TECHNICAL SPECIFICATIONS

|  |  | Reference | Value |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Declaration of performance (DOP) |  | DOPDurelisStormBlockv1 |  |  |  |  |  |
| Product type |  |  | Reinforcing construction board |  |  |  |  |
| CE class |  |  | P5 |  |  |  |  |
| Reference standard |  | EN 312 | Wood-based panel material |  |  |  |  |
| AVCP class: |  |  | 2+ |  |  |  |  |
| Certificate number |  |  | 1161-CPR-0146 |  |  |  |  |
|  |  |  | Thickness class (mm) |  |  |  |  |
| Panel material | EN13986 |  | 10 | 12 | 13 | 15 | 18 |
| Density (kg/m³) | EN323 |  | 740 | 720 | 720 | 720 | 720 |
| Bending strength (N/mm²) | EN312, table 7 |  | 18 | 18 | 18 | 16 | 16 |
| Bending stiffness (N/mm²) | EN312, table 7 |  | 2550 | 2550 | 2550 | 2400 | 2400 |
| Internal bond (N/mm²) | EN312, table 7 |  | 0.45 | 0.45 | 0.45 | 0.45 | 0.45 |
| Swelling after 24h (%) | EN312, table 7 |  | 13 | 11 | 11 | 10 | 10 |
| Moisture resistance option 1: internal bond (N/mm²) | EN312, table 8 |  | 0.25 | 0.25 | 0.25 | 0.22 | 0.22 |
| Moisture resistance option 1: thickness swelling (%) | EN312, table 8 |  | 12 | 12 | 12 | 12 | 12 |
| Formaldehyde class | EN13986, table B1 |  | E1 | E1 | E1 | E1 | E1 |
| Formaldehyde content (mg/100g) | EN120 |  | ≤ 8 | ≤ 8 | ≤ 8 | ≤ 8 | ≤ 8 |
| Reaction to fire | EN13501-1 |  | E | D-s2,d0 | D-s2,d0 | D-s2,d0 | D-s2,d0 |
| Water vapour permeability µ (wet) | EN12986, table 9 |  | 16 | 16 | 16 | 16 | 16 |
| Water vapour permeability µ (dry) | EN12986, table 9 |  | 50 | 50 | 50 | 50 | 50 |
| Moisture content (%) | EN322 |  | 6-10 | 6-10 | 6-10 | 6-10 | 6-10 |
| Airborne sound insulation (dB) | EN13986, chp 5.10 |  | NPD | NPD | NPD | NPD | NPD |
| Sound absorption (α) | EN13986, table 10 |  | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 |
| Thermal conductivity λ (W/m.K) | EN13986, table 11 |  | 0.14 | 0.14 | 0.14 | 0.14 | 0.14 |
| Strength - tension ft (N/mm²) | EN12369-1 |  | 9.4 | 9.4 | 9.4 | 8.5 | 8.5 |
| Strength - compression fc (N/mm²) | EN12369-1 |  | 12.7 | 12.7 | 12.7 | 11.8 | 11.8 |
| Strength - bending fm (N/mm²) | EN12369-1 |  | 15.0 | 15.0 | 15.0 | 13.3 | 13.3 |
| Strength - panel shear fy (N/mm²) | EN12369-1 |  | 7.0 | 7.0 | 7.0 | 6.5 | 6.5 |
| Strength - planar shear fr (N/mm²) | EN12369-1 |  | 1.9 | 1.9 | 1.9 | 1.7 | 1.7 |
| Stiffness - tension Et (N/mm²) | EN12369-1 |  | 2000 | 2000 | 2000 | 1900 | 1900 |
| Stiffness - compression Ec (N/mm²) | EN12369-1 |  | 2000 | 2000 | 2000 | 1900 | 1900 |
| Stiffness – bending Em (N/mm²) | EN12369-1 |  | 3500 | 3500 | 3500 | 3300 | 3300 |
| Stiffness - panel shear Gv (N/mm²) | EN12369-1 |  | 960 | 960 | 960 | 930 | 930 |
| Impact resistance (class) | EN12871 |  | NPD | NPD | NPD | NPD | NPD |
| Linear expansion δI30.85 (mm/m) | EN318 |  | < 3 | < 3 | < 3 | < 3 | < 3 |
| Mechanical durability (kmod;kdef) |  |  | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 |
| Biological durability (class) | EN335 |  | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 |
| Pentachlorophenol (PCP) content (ppm) | EN13986, chp 5.18 |  | < 5 | < 5 | < 5 | < 5 | < 5 |